LAMINATOR PHOTORESIST

1. The side on which your are putting the photoresist, should be facing downwards as the heating element in on the bottom in the laminator i have

2. While putting the PCB + photoresist, hold and feed the photoresist. Don't let it be just like that else it might get crumpled inside the laminator

3. Laminate each side 8-10 times to ensure the photoresist sticks to the PCB properly. When I did 3 times, the photoresist came off the PCB after exposure ir. it was not heat bonded to the PCB properly